## Slide 1: Neutron detectors: new detectors, innovative materials and new algorithms for Pulse Shape Discrimination
F. Gramegna
INFN
Laboratori Nazionali di Legnaro
ORganic scIntillators fOr NEutrons
International Workshop on Nuclear Dynamics and Thermodynamics
in Honor of Prof. Joe Natowitz
Texas A&M University, College Station, Texas, USA
August 19-22, 2013

## Slide 2
Why neutron detectors are important
Status of the art plastic and liquid scintillators advantages & drawbacks
Plastics vs Elastomers
Preparing new scintillators :
REVIEW OF FAILURES & SUCCESSES:
Selection of:
Luminescent silicone
rubber matrix
Luminescent Dye
molecules
Suitable organic compound
for B or Gd doping
Radiation hardness
Pulse Shape Discrimination
Summary

## Slide 3
A renewed interest in
Neutron Detectors development
has grown up again.
Applications:
Detectors in Nuclear Physics experiments
Monitors in high neutron flux environments (Nuclear Power Plants, Spallation Neutron Sources, RIB accelerators, Homeland Security …)
Detectors and Monitors for Nuclear Medicine. (BNCT, hadron therapy, …)
Material Analysis
Scientific Motivation
Multiple scattering by Hydrogen and Carbon
High Energy Neutrons (E>1 MeV)
Low Energy Neutrons (E<500 keV – 1 MeV)
Neutron Capture by B or Gd nuclei dissolved in the silicone rubber

## Slide 4
Liquids & Plastics
    STATUS of the ART
    Organic Scintillators:
    Liquid scintillators: high quantum efficiency, n-g pulse shape discrimination, fast response (3÷4 ns)
    Toxic, corrosive, flammable, explosive, high volatility, sensitivity to Oxygen, needs of sealing, high cost...
    (es. BC501, EJ301 etc.)
    Plastic scintillators: good quantum efficiency, different shapes and volumes, low cost, fast response (2÷ 3 ns)
    Low radiation hardness, no pulse shape discrimination, sensitivity to organic solvents (crazing)
    (es. EJ212, NE102 etc.)

## Slide 5: EJ-212 Commercial Plastic
plastic base (polyvinyltoluene)
solute 1 p-terphenyl( 1-4 % wt.)
solute 2 POPOP (≤ 0.1% wt.)
Transparent (low re-absorption)
High Quantum Efficiency (10.000 photons/MeV)
Linear response to g-radiation with energy
Fast response (low dead time)
Rigidity (not easy shaping)
Needs of optical glueing for Photo detector coupling
Undergoes radiation degrading (yellowing)
no Pulse Shape Discrimination
Plastics

## Slide 6
New Scintillators
  Avoid liquid scintillators  toxic, flammable and dangerous for the environment
  Overcome drawback of presently used plastic scintillators
  Production and characterization of new plastic scintillators based on silicone rubbers.
  Detection of low energy neutrons  doping with Gd and B also under study.
  Interest is focused on Polysiloxane based scintillators ( Z.W. Bell, et al. ., IEEE Trans. Nucl. Sci. 51 (2004) 1773- 1776. , Z.W. Bell et al., “Organic scintillators for neutron detection,” in X-Ray and Gamma-Ray Detectors and Applications IV, vol. 4784, Proc. SPIE, R. B. James, L. A. Franks, A. Burger, E. M. Westbrook, and R. D. Hurst, Eds., 2002, p. 150. ) : 
Eco-compatible
Constant physical properties 
wide range of temperature (-100 up to 250°C), while PS and PVT are plastic materials
with a glass transition temperature of about 90°C, hydrorepellent, permeable to O
Promising for the employment in harsh environments  they preserve their transparency even after 10 Mrad dose exposure, against the exposure limits (1-3 Mrad) of PS and PVT.
Physical properties can be tailored by varying the amount of phenyl groups in the chain  refractive index , thermal resistance , fluorescence
Provide fast response signals (2-3 ns)
Can be modeled in any solid shape.

## Slide 7
Si-O
C-C
    Energy (KJ/mol)
    452
    346
    Bond Length (Å)
    1.63-1.66
    1.54
    Angle (deg)
    130 - 150
    109.5
    FIX!
Stronger!!
Longer!
More Flexible!
    Torsional Barrier (KJ/mol)
    0!
    13
    VARIABLE!
    Plastics vs Elastomers: comparing polymeric structures
    Si-O (Polysiloxane) e C-C (PVT, polyethilene)
More radiation hard
ELASTOMER!!!
Courtesy of S. Carturan
poly-dimethyl-siloxane
polyethylene
Notes: .

## Slide 8
Polysiloxane based scintillators: Addition
Pt Catalyst  transition element  weakens the double bond
Reactive terminal vinyl groups – double bond
Reactive Hydride Groups Si-H
Silicone RTV: room temperature Vulcanization
polydimethyl-co-diphenyl siloxane vinyl terminated
Phenylmethylsiloxane Hydride terminated
Polymethylphenylsiloxane vinyl terminated

## Slide 9
Polysiloxane based scintillators: Condensation
Etoxy Terminal Groups
Hydroxyl Terminal Groups

## Slide 10
    Overlap between dye absorption spectrum and polymer
    fluorescence spectrum.
    Good solubility in the polymer matrix due to lateral phenil groups (PPO)
    Good radiation hardness
    2,5 diphenyloxazole
    or
    Suitable Dye Molecules: 1st Dye
butyl Phenylbutadiene
Fluorescence spectra of silicone and PPO
PPO
H6524 Hamamatsu (PMT R1450 (response spectra
350 – 600 nm))

## Slide 11: Red emitting polysiloxane based scintillators
PPO, bPBD etc.
Lumogen Violet (LV), BBOT, dPOPOP etc.
Suitable Dye Molecules: photo-sensor coupling
Phenyl substituted polysiloxane resins
2,5-Diphenyloxazole (PPO)
Lumogen Violet (LV)
Lumogen Red (LR)
Blu emitting polysiloxane based scintillators
A. Quaranta et al. Optical Materials 32 (2010) 1317–1320
Naphtalimidi  LV/LR
Luminescent dyes for promoting high luminescence yield at about 430 nm (PPO or bPBD)+(dPOPOP or LV), while
~ 600nm LR.
Boron O-carborane or Gadolinium nitrate tributylsulfate: used as thermal neutron
sensitizer.

## Slide 12
Series | 1° dye | 2° dye
S1_1:3 | PPO (0.5% : 2,0%) | LV(0.01%:0.04%)
S2_1:3 | PPO (0,5% - 1,0%) | BBOT (0.01%:0.04%)
S2_4:9 | bPBD (0,25% - 0,5%) | LV(0.01%:0.04%)
S3_1:6 | PPO (1,0% -2,0%) | LV(0.01%:0.04%)
S3_7:9 | DMT (0,35% - 2,0%) | BBOT (0.01%:0.04%)
S3_10:12 | DMT (0,35% - 2,0%) | LV(0.01%:0.04%)
S4_1:3 | bPBD (0,2%) | BBOT (0.01%:0.04%)
S5 3cm | PPO (1,0%) | BBOT (0.02%)
S6_1:7 | PPO (1,0% -2,0%) | LV(0.01%:0.04%)
LV * | PPO (1,0% - 1,5%) | LV (0.01% : 0,05%)
dPOPOP* | PPO (1,0%) | dPOPOP (0,01% - 0,02)
Sample production: Polysiloxane rubbers
PPO/dPOPOP | 1/0,01 22-100 | 1/0,01 22-100 | 1/0,02 22-100 | 1/0,02 22-100
Am-241 L.O vs EJ212 | 51%±16% | 46%±15% | 46%±15% | 45%±15%
Co-60 L.O vs EJ212 | 66%±20% | 60%±18% | 72%±16% | 65%±22%
241Am- a
NE102

## Slide 13
Light output for 241Am a-particles
    Comparison between solid samples
BBOT
DMT
LV
BBOT
b-PBD
LV
PPO
BBOT
Chart: 
| S. 1-1 | S. 1-2 | S. 1-3 | S. 2-1 | S. 2-2 | S. 2-3 | S. 2-4 | S. 2-5 | S. 2-6 | S. 2-7 | S. 2-8 | S. 2-9 | S. 3-1 | S. 3-2 | S. 3-3 | S. 3-4 | S. 3-5 | S. 3-6 | S. 3-7 | S. 3-8 | S. 3-9 | S. 3-10 | S. 3-11 | S. 3-12 | S. 4-1 | S. 4-2 | S. 4-3 | S. 5 3cm | S. 6-1 | S. 6-2 | S. 6-3 | S. 6-4 | S. 6-5 | S. 6-6 | S. 6-7 | S. 7-1 | S. 7-2 | S. 7-3 | S. 7-4 | S. 7-5 | S. 7-6 | S. 7-7 | S. 7-8 | S. 7-9 | S. 7-10 | S. 8-1 5CM | S. 8-2 | S. 8-3 | S. 8-4 (1)
 | 0.32319 | 0.26496 | 0.54717 | 0.5849 | 0.68657 | 0.5079 | 0.28825 | 0.37586 | 0.26189 | 0.48196 | 0.43751 | 0.53023 | 0.67622 | 0.69964 | 0.38232 | 0.48459 | 0.32091 | 0.50394 | 0.14146 | 0.08626 | 0.10943 | 0.21796 | 0.20994 | 0.25474 | 0.13372 | 0.07778 | 0.11634 | 0.41074 | 0.7645 | 0.67207 | 0.71606 | 0.42435 | 0.34659 | 0.68096 | 0.66185 | 0.53181 | 0.54942 | 0.68567 | 0.67136 | 0.52036 | 0.20801 | 0.18358 | 0.09201 | 0.50143 | 0.047326 | 0.046843 | 0.045719 | 0.15967 | 0.10324
BBOT
DMT
LV
BBOT
b-PBD
LV
PPO
BBOT
Light output for 60Co g-rays
PPO+BBOT
bPBD
LV
bPBD
LV

## Slide 14
    Silicone Rubber : slow neutron detection
    Choice of new organic compounds for dispersing Gd and B in the silicone polymer.
Gadolinium and Boron
compound requirements:
Highly soluble in the siloxane fluids.
Inert to the cross-linking reaction and to the light yield.
Thermally resistant (up to 100°C, final annealing for the cross-linking completion).
Gadolinium nitrate tributylsulfate:
Low yield (10 - 25 % with respect to EJ212)
Yellowing of samples
MT003 15% Phenil no PPO
MT012 15% Phenil 1.5% PPO
SB015 25% Phenil 1.0% PPO
GD021 25% Phenil 1.5% PPO, 1.0% Gd
241Am – 60 keV g-rays
AmBe Source
25% Phenil 1.5% PPO, 3.0% Gd

## Slide 15
% B | α – yield (% Ej-212) | γ – yield (% Ej-212) | α – yield (% Ej-254) | γ – yield (% Ej-254)
no | 65 ± 16 | 74 ± 15 | - | -
4 | 44 ± 13 | 49 ± 12 | 66 ± 22 | 69 ± 16
6 | 40 ± 14 | 48 ± 11 | 64 ± 24 | 69 ± 15
8 | 37 ± 13 | 41 ± 17 | 59± 20 | 62± 20
with termalization
Boron O-carborane
Boron Doped Polysiloxane scintillators properties:
A22_1%PPO_0.01%dPOPOP
Mixing of A :Polydimethyl-diphenyl siloxane (22%ph groups)
with B: Polymethyl phenyl Siloxane
(100%ph groups)
Addition Resins results:
EJ254
PS_B6%
n


## Slide 16
Boron Doped Polysiloxane scintillators properties:
4% B
6% B 8% B
Light output with a- particles in % of EJ-212 as a function of time. No ageing effects are visible.
Samples without B exhibit a scintillation yield 60-70% with respect to EJ-212.
Increasing the amount of B slightly affects the scintillation yield slightly less than the commercial (see EJ254).
Ageing effects
B concentrations higher (up to 8% than commercial systems (5% max. in EJ-254) can be attained, thus increasing the detection efficiency to thermal neutrons.
Base Resin | Acond 100:20:1 | Acond 100:20:1 | Acond 100:20:1 | Acond 100:20:1
PPO | 1 | 1 | 1 | 1
LV | 0,02 | 0,01 | 0,02 | 0,02
natB | NO | 4% | 5% | 6%
241Am %L.O vs EJ212 %L.O vs EJ254 | 56±16 | 49±15 73±25 | 42±13 63±22 | 48±15 71±24
60Co %L.O vs EJ212 %L.O vs EJ254 | 68±15 | 70±17 90±22 | 61±15 79±20 | 68±15 87±19
A: 100 % resin Sylanole terminated
B: 20% polydiethoxysilane (PDS)
1% Sn catalyst
Condensation Samples
Light Output

## Slide 17
Good chemical and thermal stability
Manufacturability and low cost (about 1 €/g)
No volatile solvents
Low toxicity
Very good radiation hardness
stable from -100 to +200 °C
60Co g-rays irradiated commercial PVT based scintillator
60Co g-rays irradiated polysiloxane scintillator
A. Quaranta, S. Carturan, et al., Mater. Chem. Phys., 137 (2013) 951.
Polysiloxane based scintillators: performances
241Am a-particle relative Yield
Optical transmittance spectra for EJ212 and Polyphenyl Siloxane with dye (1%PPO. 0.02LV) before and after exposure to 54KGy dose

## Slide 18
Radiation Hardness
In doped polysiloxanes the radiation hardness depends on the dispersed dye.
Samples containing Lumogen Violet are intrinsically more resistant than EJ212 and BBOT containing scintillators.
A. Quaranta et al. Nuclear Instruments and Methods in Physics Research B 268 (2010) 3155–3159
Irradiation fluence He+ @1.8 MeV (1. 0 mA/cm2)

## Slide 19
Light Output
Time
Total
Fast Component
Slow Component
Pulse Shape Discrimination
N. Zaitseva et al., NIMA668(2012)88-93
PVT

## Slide 20
Polymethylphenyl Siloxane (A-Add100) | LV 0,02% | Variable PPO 1%,2%,3%,4%,5%,6%. Variable bPBD 0,1%,0,2%,0,3%,0,5%,1% | Polymethylphenyl dimethyl siloxane (B-Add) | Platinum 1,2μL/g + Inhibitor 6μL/g
Polydimethyl diphenyl siloxane (A-Add22) | LV 0,02% | Variable PPO 1%,2%,3%. bPBD variabile 0,1%,0,2%,0,3%, 0,4%,0,5%,1% | Polymethylphenyl dimethyl siloxane (B-Add) | Platinum 1μL/g + Inhibitor 6μL/g
OH terminated Siloxane (A-Cond18) | LV 0,02% | Variable PPO 1%,2%,3%,4%,5%,6%. Variable bPBD 0,1%,0,3%,0,5%. | Polydiethoxysilane (PDS, B-Cond) | Tin 1,3%.
Resin (A) | Dye | Resin (B) | Catalyst
Sample production: Polysiloxane rubbers
Add-100
Add-22
Cond-18

## Slide 21
%YIELD (VS EJ212)
% b-PBD
% B-PBD
Solubility limit
    Comparison between solid samples
%b-PBD
%YIELD (VS EJ212)
%b-PBD
b-PBD
b-PBD

## Slide 22
%YIELD vs EJ212
%YIELD vs EJ212
    Comparison between solid samples

## Slide 23
Neutron/gamma discrimination: Zero crossing method
RC/CR emulation algorithm provided by L. Bardelli:
[L. Bardelli et al., Nucl. Instr. and Meth., A521 (2004) 480]
Pulse Shape Analysis: using standard scintillators (BC501)
beam
Time
pickup
n
PM1
PM2
Digital Electronics
CAEN Digitizers |  |  | 
Model | S. rate | D. Range | Res
V1720 | 250 MS/s | 2 Vpp | 12 bit
V1751 | 1 - 2 GS/s | 1 Vpp | 10 bit
target

## Slide 24
Pulse Shape Analysis: large samples (Ø=3”)
ToF Spectra CN measurement
Average Shapes: neutron/Alpha/Gamma discrimination V1751 CAEN 1GS/s 10 bit 1Vpp
PS_PPO1(n-a g)
PS_PPO8 (n- g)
PS_PPO1_B3(n-a g)

## Slide 25
Pulse Shape Analysis: small samples (Ø=0.8”)
Average Shapes small samples : Alpha/Gamma discrimination 1GS/s 10 bit 1Vpp
EJ212-a ,EJ212 - g
p-terphenyl( 1-4 % wt.)
g-rays
a
PPO1,2,4,6,8%
PPO1,2,4,6,8%
EJ212-a ,EJ212 - g,
PS_PPO8 - a,PS_PPO8 - g
EJ212-a ,EJ212 - g,
PS_PPO1 - a,PS_PPO1 - g
g
a

## Slide 26
Pulse Shape Analysis: large samples (Ø=3”) – fast vs slow
Average Shapes: neutron/Alpha/Gamma discrimination V1720 CAEN 250MS/s 12 bit 2Vpp
PS_PPO1(n- g)
PS_PPO8(n- g)
PS_PPO1(n- g)
n
g
PS_PPO8(n- g)
n
g
PS_PPO8(n- g)

## Slide 27
Aim: substitution of Benzen (highly toxic, inflammable, dangerous handling)
Sample production: liquid scintillators
Polymethylphenyl siloxane (100%) | 10 cSt | PPO 1%,2% o p-TerPhenyl 0,1%,0,5% | LV 0,02%
Polymethylphenyl dimethyl siloxane(48%) | 125 cSt | PPO 1%,2% o p-TerPhenyl 0,1%,0,5% | LV 0,02%
Polymethylphenyl dimethyl siloxane(56%) | 500 cSt | PPO 1%,2% o p-TerPhenyl 0,1%,0,5% | LV 0,02%
Matrix | Viscosity | Dye
Preliminary

## Slide 28
Molar % of benzenic groups
Molar % of benzenic groups
Growth as a function of n. of benzenic groups
2% PPO
1% PPO
%YIELD vs EJ212
%YIELD vs EJ212
Sample production: liquid scintillators
Preliminary
2% PPO
1% PPO

## Slide 29
Development of blue and red emitting polysiloxane based scintillators  improved spectral matching with PMT & APD detectors
Energy transfer investigation and emission intensity optimization by fluorescence spectroscopy and scintillation measurements with/without optical filters with PMT under radiation sources or accelerated beams.
A22 & A100 with PPO & LV show optimum quantum efficiency (50-60% vs EJ212), optimum reproducibility, no ageing effects, radiation hard.
New solid samples: A18 COND optimum transparency, dye solubility, optimum light yield (up to 60-70% vs EJ212), also when B loaded.
Preliminary new liquid scintillators: Atoxic, optimum Dye solubility, light yield get better at the growing of Benzenic groups, optimum light output (up to 70% vs EJ212)
Preliminary PSA discrimination: average shapes are sensitive to incoming radiation at contrary of EJ212- Alghoritms still to be optimized
SUMMARY

## Slide 30
Outlooks: Hyde
Si p-type
P diffuse (n+)
nitride
oxide
Electric contacts
(n+)
Signal pick up
    p
    a
    10B
scintillator
    Fast n
    Slow n
SiPM
    3D silicon detector
    PS scintillator
No Silicone
Converter
with Silicone
Converter
200 m
10 m

## Slide 31: The ORIONE Collaboration:
S. Carturan1,2, F. Gramegna1, M. Cinausero1 , G. Collazuol1,2 , M. Dalla Palma1,3, M. Degerlier4, T. Marchi1,2, A. Quaranta1,3 .
1 INFN, Laboratori Nazionali di Legnaro, Legnaro (Pd), Italy.
2Department of Physics and Astronomy, University of Padova, Padova, Italy.
3Department of Industrial Engineering, University of Trento, Trento, Italy.
4Department of Physics, University of Nevsehir, Nevsehir, Turkey .
The Collaborations
NEutron DEtector developments for Nuclear Structure, Astrophysics and Applications (NEDENSAA) NuPNET - Network
    Italy (INFN - LNL, LNS).
    Germany (TU Dresden).
    France (CNRS/IN2P3, CEA, DRT, LIST, DCSI, LCAE).
    Spain (CIEMAT, IFIC).
    Finland (Univ. Jyväskylä).
    Bulgaria (INRNE).
    Turkey (TUBITAK)
    Sweden (Univ. Uppsala).
The HYDE Collaboration
ORIONE Collaborators plus:
G. Dalla Betta1 & Coworkers
M. Boscardin 2 & Coworkers
G. Susinno3 & Coworkers
1Department of Industrial Engineering ,
University of Trento, Trento, Italy.
2FBK (Bruno Kessler Foundation), Trento
3 INFN & Department of Physics, University of Calabria, Cosenza, Italy .

## Slide 32
Best Wishes JOE !!!!!!!!!!!!

## Slide 33
BACKUP
SLIDES

## Slide 34
X-ray diffraction patterns
NO sharp peaks → NO 3-D crystalline order
Negligible changes with aging
Negligible changes with polymerization routes
Two components: intense and sharp peak at 10.7° and a hump at about 19.7°
  19.7° Si-O-Si amorphous phase of silica-like structure in siloxane
  10.7° ordered domains (lamellae with folded chains) without close crystalline packing
Ribbon-like structure of PDMS with unit cell
J.J.H. Lancastre et al., Rad. Chem. Phys., 2012
Courtesy of G. Maggioni

## Slide 35
Multiple scattering by Hydrogen and Carbon
High Energy Neutrons (E>1 MeV)
Low Energy Neutrons (E<500 keV – 1 MeV)
Neutron Capture by B or Gd nuclei dissolved in the silicone rubber
Interaction processes a new working detector
Study and production of new polysiloxane organic scintillators (PSS) for neutrons detection.
Naphtalimidi
LV/LR
PPO
POPOP
Luminescent dyes for promoting high luminescence yield at about 430 nm (PPO or bPBD)+(dPOPOP or LV, LR).
Matrix
Boron O-carborane or Gadolinium nitrate tributylsulfate: used as thermal neutron sensitizer.
DMT
Dimethyltryptamine
Notes: Our study is devoted to develop new detectors able to be used both for fast and for thermal neutron detection. Fast neutrons are known to interact with organic matrials through their elastic or inelastic interaction with the C or H atoms. On the contrary slow neutrons, especially in the thermal region, mainly interact by capture reactions with special materials which are interesting due to their high capture cross section: among them very common are the n-capture on 10B, with the emission of a correlated couple made by an alpha particle and a Li ion , while in the case of Gd (much higher cross section) the emission are gammas and a characteristic X rays of 42 keV.
To produce a scintillator the base organic resin must be a scintillator (emit light) and it must be added with different amounts of fluorophores to transfer the enrgy of the emitted radiation in the visible region. As primary dye organic composites like 2,5-diphenyloxazole (PPO) or butyl PhenilButadiene (bPBD) has been used, while dPOPOP or Lumogen Violet (registered Trademark of BASF) were used as wavelength shifter as I will discuss later. Ortho-carborane or Gadolinium nitrate tributylsulfate have been added as neutron sensitizer in the base resin before the cross-linking reaction for those samples to be used for thermal neutron detection.

## Slide 36
From Shapes to parameters: fast vs slow with squared-root.
241Am
PPO1%
60Co
PPO8%
60Co
PPO1%
PPO8%
PPO1%
PPO8%
1GS/s 10 bit
250MS/s 12 bit

## Slide 38: BBOT
Assorbe 370 nm (UV)
Emette 430 nm (viola)
430 nm
370 nm

## Slide 39
Light emission and wl.-shifting (PPO/BBOT)
Conclusion
PPO/BBOT scitntillation and light detection
γ, X absorption
B neutron capture and α emission
Low Energy Neutrons
Gd neutron capture and γ o X emission
 absorption
“transparency ”X ray detection
-Light Yield measurements with α and γ sources.
-IBIL measures.
-Neutron Source tests.
-TOF measures.

## Slide 40
Light Yield Measurement – γ sources
γ
γ
Tommaso Marchi – tommaso.marchi@lnl.infn.it
1-dec-2009: NEDA technical meeting

## Slide 41: Scintillatori organici (solidi)
Gli scintillatori organici sono formati da idrocarburi aromatici (contenenti anelli benzenici) in forma di polimero.
In questi composti la fluorescenza deriva da transizioni degli elettroni delocalizzati dell’anello benzenico.

## Slide 42: Light
400 nm
750 nm
IR
UV

## Slide 43: Scintillation process
Primary Phase:
Radiation Absorption
excitation (or ionization) of molecules
Second Phase :
Internal conversion
energy transfer
Light emission (or quenching)

## Slide 44: Decay
Fluorescence (10 ns-100 μs)
Phosphorescence
(>100 μs)
Vibrational De-excitation
Emission h
Emission h
S0
S1
T1
Absorption h
Absorption h

## Slide 45: Fluorescence

## Slide 48
Chart: Light Output relative to EJ212 –a-particles for B doped samples
| PPO(%)1 e BBOT(%) 0,02 e B(%) 1 | PPO(%)1 e BBOT(%) 0,02 e B(%) 2 | PPO(%)1 e BBOT(%) 0,02 e B(%) 3 | PPO(%)1 e BBOT(%) 0,02 e B(%) 4 | PPO(%)1 e BBOT(%) 0,02 e B(%) 5
Particelle alfa scintillatori con boro | 0.2458 | 0.21618 | 0.16711 | 0.35721 | 0.10743
Chart: Light Output relative to EJ212 – a-particles
| PPO(%)1 e BBOT(%) 0,01 | PPO(%)1 e BBOT(%) 0,015 | PPO(%)1 e BBOT(%) 0,02 | PPO(%)1 e BBOT(%) 0,03 | PPO(%)1 e BBOT(%) 0,04 | PPO(%)2 e BBOT(%) 0,01 | PPO(%)2 e BBOT(%) 0,02 | PPO(%)2 e BBOT(%) 0,04
Particelle alfa scintillatori senza boro | 0.51633 | 0.47636 | 0.59513 | 0.13738 | 0.44686 | 0.57591 | 0.55102 | 0.56894
    Comparison between solid samples